## Slide 1: Advanced Details for Adjacent Box Beam Connections
Ben Graybeal, Ph.D., P.E.
Team Leader – Bridge & Foundation Engineering
Federal Highway Administration
202-493-3122
benjamin.graybeal@dot.gov
Iowa DOT ABC Workshop — May 1-2, 2014

## Slide 2
Considerations…
Acceptability/Unacceptability of current practice
Weaknesses to be addressed
Economic considerations
Bounds of new solution

## Slide 3: Objective
Enhance performance of adjacent box beam bridges
Focus on longitudinal connection details
  Assess common connection details
  Develop advanced connection details

## Slide 4: Field-Cast “Splice” Connections
Simple Lap-Splice Cxn
Smaller Grout Volumes
Shortened Bar Lengths
Emulates Monolithic Component

## Slide 5: Field-Cast “Splice” Connections
Precast Deck Panels
and Slabs
Deck Bulb Tee Girders

## Slide 6: Adjacent Box Beam Connections

## Slide 7: Adjacent Box Beam Connections
Traditional Solution w/ Post-Tensioning
UHPC Connection Solution w/o Post-Tensioning

## Slide 8
Conventional Shear Key
Post-Tension

## Slide 9
UHPC Connection
No. 4 rebar lap splice
(No Post-Tension needed)
Embedded Length: 5.5 in.
Lap spliced Length: ≈ 4in.

## Slide 10
Surface Finishes

## Slide 11: Adjacent Box Beam Connections
Loading

## Slide 12: Adjacent Box Beam Connections

## Slide 13
Four Points Bending
Cross Section
Elevation
Off Center 6 in.
Simply Supported

## Slide 14
Loading Range: 18, 36, 54, 72, 90 kips
Test Setup
Loading Protocol #1 (Simply Supported)
Equivalent to the distributed load from a fatigue truck

## Slide 15
Four Points Bending
Cross Section
Elevation
Off Center 6 in.
Test Setup
Restrained Deflection

## Slide 16
Pull down force
Test Setup
Restrained Rotation at Ends

## Slide 17
Pull down force
Support
Beam 2
Beam 1
shear key
Test Setup
Restrained Deflection at Diaphragms

## Slide 18
Loading Range: 18, 36, 54, 72, 90 kips
Test Setup
Loading Protocol #2 (Restrained Deflection)

## Slide 19
Thermal loading caused no distress
Traffic loading appears unlikely to initiate new cracks
Traffic loading will cause crack growth
Transverse PT has minimal effect before cracking
Transverse PT cannot stop crack growth
Conventional grouted keys can perform well
  Must avoid cracks (shrinkage, surface prep, etc.)
Conventional Grouted Shear Keys:

## Slide 20
UHPC connections create a robust reinforced system
No distress generated in UHPC connections
UHPC Shear Keys:

## Slide 21
Cracking the Connection

## Slide 22: Conventional Grout & Partial Depth: Crack at the interface
Conventional Connection
Observation: Transverse PT does not stop crack propagation

## Slide 23
Cyclic structural loads did not initiate cracks
Under forced cracking → crack in box beam
UHPC Connection w/o PT
Connection

## Slide 24
Full-Depth Conventional Grout
Beam A
Beam B
Beam A
Beam B
Transverse force
(a)
(b)

## Slide 25: Sollars Road Bridge

## Slide 26: Sollars Road Bridge

## Slide 27: Sollars Road Bridge

## Slide 28: Sollars Road Bridge

## Slide 29: Sollars Road Bridge

## Slide 30: Sollars Road Bridge

## Slide 31: Sturgeon River Bridge

## Slide 32: Sturgeon River Bridge

## Slide 33: Sturgeon River Bridge

## Slide 34
Considerations…
Acceptability/Unacceptability of current practice
Weaknesses to be addressed
  Connection Deterioration? Differential Movement? Corrosion?
Economic considerations
Bounds of new solution
  PT or No PT? Surface Preparation? UHPC? GFRP?

## Slide 35: Advanced Details for Adjacent Box Beam Connections
Ben Graybeal, Ph.D., P.E.
Team Leader – Bridge & Foundation Engineering
Federal Highway Administration
202-493-3122
benjamin.graybeal@dot.gov
Iowa DOT ABC Workshop — May 1-2, 2014

## Slide 36
Guidance on Use of UHPC Connections
FHWA document being drafted
  Design guidance
  Construction guidance
  Case Studies
Publication within 6 months
External reviews underway