## Slide 1: UHPC for PBES Connections: A Path to Accelerated Construction and Enhanced Bridge Performance
Ben Graybeal, Ph.D., P.E.
Team Leader – Bridge & Foundation Engineering
Federal Highway Administration
202-493-3122
benjamin.graybeal@dot.gov
Iowa DOT ABC Workshop — May 1-2, 2014

## Slide 2: Performance
Longevity
Sustainability
Serviceability
Strength
Cost-Effectiveness
Resiliency

## Slide 3: Prefabrication
Connections
Connections
Connections

## Slide 4
Must be: – Robust, Ductile, Durable
Frequently: – Emulative
PBES Connections

## Slide 5
Must be: – Robust, Ductile, Durable
Frequently: – Emulative
PBES Connections
What we need: – Strong, Durable Material – Good Bond to Concrete – Good Bond to Rebar
– Self Consolidating
– Sustained Tensile Strength
– Short Development Length

## Slide 6
What we need: – Strong, Durable Material – Good Bond to Concrete – Good Bond to Rebar
– Self Consolidating
– Sustained Tensile Strength
– Short Development Length
PBES Connections

## Slide 7: Solution:
What we need: – Strong, Durable Material – Good Bond to Concrete – Good Bond to Rebar
– Self Consolidating
– Sustained Tensile Strength
– Short Development Length
UHPC
PBES Connections

## Slide 8: What is Ultra-High Performance Concrete?
ACI 239 – Ultra-High Performance Concrete
  Concrete, ultra-high performance - concrete that has a minimum specified compressive strength of 150 MPa (22,000 psi) with specified durability, tensile ductility and toughness requirements; fibers are generally included to achieve specified requirements.

## Slide 9: What is Ultra-High Performance Concrete?
Advanced cementitious composite material
High strength, high stiffness
Exceptional durability
Internal steel fiber reinforcement for added ductility
Self-consolidating
150+ MPa Compression
5+ MPa Tension
Fiber Reinforced
Self-Consolidating
Low Permeability

## Slide 10
Introduction to UHPC
NHI Innovations Webinars – November 18, 2010 and April 21, 2011
FIU ABC Webinar – September 29, 2011
TechNote: UHPC
  FHWA HRT-11-038
  Aimed at DOTs and practitioners
  General information on casting, curing, testing, applications, inspection, etc.
  Web Search: UHPC TechNote

## Slide 11
UHPC State-of-the-Art Report
FHWA HRT-13-060
  300+ references
  600+ item bibliography
  Materials, Performance, Design, Applications, Outlook
  Web Search: UHPC State of the Art

## Slide 12
FHWA UHPC Memo – 12 Feb 2014
Buy America re: Fibers
Availability
Proprietary Products
Example Special Provision (NYSDOT)

## Slide 13: Non-Proprietary UHPC
Full Report on Study Results
Report: NTIS PB2013-110587
TechBrief: FHWA HRT-13-100

## Slide 14
FHWA UHPC Website
https://www.fhwa.dot.gov/research/resources/uhpc/
Web Search: UHPC FHWA
Overview, Research Projects, Bridges, Publications

## Slide 15: UHPC Connections
Deck-to-Deck
Deck-to-Girder
Column-to-Footing/Cap
Girder-to-Girder
Deck-to-Barrier
Deck-to-Expansion Joint

## Slide 16
TechNote: UHPC Connections
FHWA HRT-12-038
  Aimed at DOTs and practitioners
  General information on field-cast use of UHPC
  Web Search: UHPC Connections TechNote

## Slide 17: Field-Cast “Splice” Connections
Simple Lap-Splice Cxn
Smaller Grout Volumes
Shortened Bar Lengths
Emulates Monolithic Component

## Slide 18: Field-Cast “Splice” Connections
Precast Deck Panels
and Slabs
Deck Bulb Tee Girders

## Slide 19
Deck-Level UHPC Connections
Notes: The photo shows panel B1/B2 under cyclic load. The pond can be seen on the surface of the panel.

## Slide 20
Slab/Plate/Deck Connections w/ UHPC
Field-Cast, Non-Contact Lap Splice Connection
6” (152 mm)
6” (152 mm)
5.9” (150 mm)
LAP
8” (203 mm)
5.9” (150 mm)
1”
(25 mm)
1.5”
(38 mm)

## Slide 21: Deck-Level UHPC Connections
Full Report on Study Results
Report: NTIS PB2011-101995
TechBrief: FHWA HRT-11-022

## Slide 22
4-point bending test
High-cycle fatigue then static to fail
Panel-to-Panel UHPC Connections

## Slide 23
22 panel-to-panel connections w/ UHPC
#5 bars lap-spliced 5.5” in 6” wide connection
Considered bar type, lacers, interface prep
2M+ cycles fatigue; static to failure
Results:
No failures in UHPC connections.
Observed failure modes – conventional concrete crushing
steel rebar fatigue
steel rebar yielding / fracture

## Slide 24: Seismic Testing of a Deck-Bulb-Tee Connection

## Slide 25: Seismic Testing of a Deck-Bulb-Tee Connection
University of Buffalo

## Slide 26: Column-to-Footing/Cap Connections
University of Nevada-Reno

## Slide 27
Seismic Design of PBES Systems
Emulative connections are possible with UHPC
  Constructible, cost-effective, and robust
Connections can be located away from hinge regions
Connections may have locally higher stiffness
Connections in plate elements, walls, and/or plates-to-beams are entry points for technology adoption

## Slide 28: Field-Cast Deck-to-Girder Connections
Simple Connection
No Interference
Hidden Connection
Emulates Cast-in-Place

## Slide 29: Field-Cast “Interface” Connections

## Slide 30
UHPC Composite Cxn Test

## Slide 31
UHPC Composite Connection
Steel Girder Connection
Concrete Girder Connection

## Slide 32: Composite Connections for Precast Deck Panels

## Slide 34: Composite Connections for Precast Deck Panels
Full Report on Study Results
Report: NTIS PB2012-107569
TechBrief: FHWA HRT-12-042

## Slide 35: Adjacent Box Beam Connections

## Slide 36: Adjacent Box Beam Connections

## Slide 37: Adjacent Box Beam Connections
Traditional Solution w/ Post-Tensioning
UHPC Connection Solution w/o Post-Tensioning

## Slide 38: PBES Research at TFHRC
Vertically Integrated Research
  Material Performance
  Component Performance
  Structural Performance

## Slide 39: PBES Research at TFHRC
Vertically Integrated Research
  Material Performance
  Component Performance
  Structural Performance
Developing Solutions

## Slide 40
Rebar Anchorage / Splice

## Slide 41
Rebar Development Length

## Slide 42: Parameters :
Type of Grout: UHPC, Epoxy, Conventional
Type of Rebar: High-Strength, Black, Epoxy, GFRP
Embedded length/spliced length
Clear spacing to adjacent bar
Side cover
Grout strength
UHPC fiber content

## Slide 43
Effect of Embedment Length
Notes: All data points are A1035 bars, size #5. Sets 1, 3, 4 have UHPC compressive strength of approximately 13.5 ksi. Set 2 has UHPC compressive strength of 19 ksi.

## Slide 44
More than 200 tension-tension pullout tests
Conventional Concrete:
Given: = 70 ksi, = 13 ksi
ACI 318 24
AASHTO 28
UHPC 1 day strength

## Slide 45: Preliminary Findings on UHPC:
Black Rebar: 6db embedment for 60 ksi (yield)
UHPC at 13.5 ksi (1 day); 2db side cover
Epoxy Rebar: 8db embedment for 60 ksi (yield)
UHPC at 13.5 ksi (1 day); 2db side cover
Black, Epoxy Rebar: 10db embedment for rupture
UHPC at 19.5 ksi (7 day); 2db side cover
High Strength Rebar: 12db embedment for rupture
UHPC at 19.5 ksi (7 day); 2db side cover

## Slide 46: Design Recommendation
Embedment Length, ld: 8db
Side cover: 3db
Bar spacing: between 2db and ls
ls ≥ 0.75 ld
f’c ≥ 13.5 ksi
Relevant for: 1) uncoated or epoxy coated bars, and 2) No.4 to No. 8 bars.
Bar stress of at least 75 ksi before bond failure
UHPC 1 day strength

## Slide 47: Grout Characterization

## Slide 48
Chart: Time (Days after Mix Initiation)
 | 0 | 0

## Slide 49: Grout Characterization
Full Report on Study Results
Report: NTIS PB2013-130231
TechBrief: FHWA HRT-13-042

## Slide 50: PBES Innovation

## Slide 51: PBES Innovation
I-81 in Syracuse NY ─ August 2013
Acknowledgements:
NY Accelerated Bridge Program
NYSDOT
Fort Miller Group, Inc.
Slate Hill Constructors, Inc.
Economy Paving Company, Inc.

## Slide 53
NYSDOT Requirements
  Complete redecking
  10-day max closure
  No overlay…Grinding OK
  Prefabricated Barriers
  May use UHPC connections
  Exposed aggregate interfaces

## Slide 54
Precaster and General Contractor Developed the Details of the System
  Element Weight < 15 tons
  Element Length < 26 feet
  No Prestressing or PT
  Inverted Cast w/ Integrated Barrier
  Exposed Aggregate
  UHPC Connections
  ½” Sacrificial Surface…Ground

## Slide 61
Conventional Grout

## Slide 62
Field-Cast UHPC

## Slide 63
Haunch & Panel Support

## Slide 64
Deck-to-Deck Connection

## Slide 65
Deck-to-Deck Connection

## Slide 66
Deck-to-Deck Connection

## Slide 67
Deck-to-Girder Connection

## Slide 68
Deck-to-Girder Connection

## Slide 69
Deck-to-Girder Connection

## Slide 70
Deck-to-Girder Connection

## Slide 71
Deck-to-Girder Connection

## Slide 72
Deck-to-Girder Connection

## Slide 73
Deck-to-Girder Connection

## Slide 74
Deck-Barrier Components

## Slide 75
Deck-Barrier Components

## Slide 76
Deck-Barrier Components

## Slide 77
Link Slab

## Slide 78
Link Slab

## Slide 79
Riding Surface

## Slide 80
Name | Year
Mars Hill Bridge, Wapello County, IA | 2006
Route 624 over Cat Point Creek, Richmond County, VA | 2008
Jakway Park Bridge, Buchanan County, IA | 2008
State Route 31 over Canandaigua Outlet, Lyons, NY | 2009
State Route 23 over Otego Creek, Oneonta, NY | 2009
Little Cedar Creek, Wapello County, IA | 2011
Fingerboard Road Bridge over Staten Island Expressway, NY | 2011-2012
State Route 248 over Bennett Creek, NY | 2011
U.S. Route 30 over Burnt River and UPRR bridge, OR | 2011
U.S. Route 6 over Keg Creek, Pottawatomie County, IA | 2011
Ramapo River Bridge, Sloatsburg, NY | 2011
State Route 42 Bridges (2) near Lexington, NY | 2012
State Route 31 over Putnam Brook near Weedsport, NY | 2012
I-690 Bridges (2) over Peat Street near Syracuse, NY | 2012
I-690 Bridges (2) over Crouse Avenue near Syracuse, NY | 2012
I-481 Bridge over Kirkville Road near Syracuse, NY | 2012
Windham Bridge over BNSF Railroad on U.S. Route 87 near Moccasin, MT | 2012
State Route 12 over Spring Brook near Greene, NY | 2013
State Route 10 over Webster Brook near Dehli, NY | 2013
State Route 38 over Wilson Creek near Newark, NY | 2013
State Route 962G over U.S. Route 17 in Owego, NY | 2013
State Route 907W over U. S. Route 1 in Pelham, NY | 2013
State Route 2 Bridges (2) over SR9 in Colonie, NY | 2013
I-81 Bridges (2) over E Castle St in Syracuse, NY | 2013
I-81 Bridges (2) over E Calthrop Ave in Syracuse, NY | 2013
I-84 Bridges (2) over Dingle Road in Southeast, NY | 2013
I-690 Westbound over Onandaga Creek in Syracuse, NY | 2013
I-690 over N. Salina Street in Syracuse, NY | 2013
Bridges in Service in the U.S.

## Slide 81
Name | Year
Sherbrooke Pedestrian Overpass, Quebec | 1997
Highway 11 over CN Railway at Rainy Lake, Ontario | 2006
Glenmore/Legsby Pedestrian Bridge, Calgary | 2007
Highway 11/17, Sunshine Creek, Ontario | 2007
Highway 17, Hawk Lake, Ontario | 2007-2008
Sanderling Drive Pedestrian Overpass, Calgary | 2008
Highway 105 over Buller Creek, Ontario | 2009
Highway 71 over Log River, Ontario | 2009
Route 17 over Eagle River, Ontario | 2010
La Vallee River Bridge, Ontario | 2010
Highway 105 over Wabigoon River, Ontario | 2010
Highway 105 over the Chukuni River, Ontario | 2010
Steel River Bridge on Highway 17, Ontario | 2010
Mathers Creek Bridge on Highway 71, Ontario | 2010
Noden Causeway on Highway 11, Ontario | 2010-2013
Highway 17 over Current River, Ontario | 2011
Mackenzie River Bridges (2) on Highway 11/17, Ontario | 2011
Wabigoon River Bridge on Highway 605, Ontario | 2011
Whiteman Creek Bridge on Highway 24, Ontario | 2011
Shashawanda Creek Bridge, Ontario | 2011
Hodder Ave Overpass over Highway 11/17, Ontario | 2012
Hawkeye Creek Bridge on Highway 589, Ontario | 2012
Hawkeye Creek Tributary Bridge on Highway 589, Ontario | 2012
Black River Bridge on Highway 17, Ontario | 2012
Beaver Creek Bridge on Highway 594, Ontario | 2012
Middle Lake Bridge on Highway 17A, Ontario | 2012
Bridges in Service in Canada

## Slide 82
Pulaski Skyway Newark, New Jersey

## Slide 83
Guidance on Use of UHPC Connections
FHWA document being drafted
  Design guidance
  Construction guidance
  Case Studies
Publication within 6 months
External reviews underway

## Slide 84: UHPC for PBES Connections: A Path to Accelerated Construction and Enhanced Bridge Performance
Ben Graybeal, Ph.D., P.E.
Team Leader – Bridge & Foundation Engineering
Federal Highway Administration
202-493-3122
benjamin.graybeal@dot.gov
Iowa DOT ABC Workshop — May 1-2, 2014